SECTION 09855 – NOISE S.T.O.P. FABRISORB DECORATIVE ACOUSTICAL WALL PANELS

GENERAL

SUMMARY

Section includes shop-fabricated, acoustical wall panels with decorative [fabric] [vinyl] facings.

SUBMITTALS

Product Data:  For each type of core and facing material, and mounting indicated.

Samples:  For each type of core and facing material, and mounting indicated assembled in panels approximately 6 by 6 inches.

WARRANTY

Warranty Period:  One year.

PRODUCTS

MANUFACTURERS

NOISE S.T.O.P. FABRISORB  Decorative Acoustical Wall Panels:

Decorative Fabric Wrapped Custom Acoustical Wall Panels by Acoustical Surfaces, Inc.

123 Columbia Court North Suite 210.

Chaska, MN  55318

(952) 448 – 5300.

www.AcousticalSurfaces.com

Or equal.

NOISE S.T.O.P. FABRISORB DECORATIVE ACOUSTICAL WALL PANELS

Panel Materials:

Core Material: 6 to 7 lb. density glass fiber.

Core Thickness: [1 inch] [1-1/8 inch] [2 inch] [2-1/8 inch].

Sizes: [2 by 4 feet] [Custom sizes as indicated on Drawings].

Mounting:  [Adhesive Mounting] [Magnetic Fasteners] [Hook and Loop Fasteners] [Concealed Splines] [Mechanical Clips] [Impaling Clip].

Edge Details:  [Square] [Radius] [Bevel] [Half Bevel].

Edge Treatments: [Chemically Hardened] [Soft].

Acoustical Properties for 6 to 7 pcf glass fiber:

For 1 inch thickness: NRC of 0.85,

For 2 inch thickness: NRC of 1.15.

Fire Resistance: This pattern meets the requirements of National Fire Protection Association (NFPA) Class A or 1.

Flame Spread: 15.

Smoke Developed: 40.

Vinyl Facing Materials:

Type: Web core microperforated.

Style and Color: As selected by Architect from manufacturer’s standard selection.

Total Weight (oz./lin. yd.) 54" width average: 12.0.

Total Weight (oz./lin. yd.): 8.0.

Vinyl Weight (oz./lin. yd.): 5.0.

Fabric Weight (oz./lin. yd.): 3.0.

Fabric type and count: Polyester Sheeting (22 x 26).

Total average thickness: 0.018.

Light Reflectance Value (LR Value) is reported as average percent reflectance as measured by ASTM E-97 test method.

Web Core was applied to 1" thick 7 PCF rigid acoustical fiberglass on a #4 mounting and tested for noise reduction coefficient. The result was 0.80 NRC.

This pattern satisfactorily passes physical requirements for type I as listed in G.S.A. Federal Specification CCC-W-408A. (Federal Specification CCC-T-191 details test procedures required.)

Fire Resistance: This pattern meets the requirements of National Fire Protection Association (NFPA) Class A or 1.

Flame Spread: 20.

Smoke Developed: 65.

Stain Resistance:  (ASTM D-1308, METHOD B-24 hour exposure followed by washing with soap and water.)

Fabric Facing Materials:

Type: Guilford FR 701 2100 Fabric Facings.

Style and Color: As selected by Architect from manufacturer’s standard selection.

Fire Resistance: This pattern meets the requirements of National Fire Protection Association (NFPA) Class A or 1.

Flame Spread: 5.

Smoke Developed: 70.

Attachment Materials:

Adhesive: AGS-29 or PSA-29 panel adhesive.

Hook & Loop fasteners.

Mechanical clips.

Impaling clips.

Magnetic clips.

Splines.

EXECUTION

INSTALLATION

General: Comply with decorative acoustical wall panel manufacturer's written instructions for installation and type of mounting specified.

ADHESIVE MOUNTING

Panels are to be installed per recommended adhesive instructions.

MAGNETIC FASTENERS

The magnetic fastener is applied to the panel before shipment. Permanent spanport is required

HOOK AND LOOP FASTENERS

The loop side of the fastener is applied to the panel at time of shipment. The hook side is attached to its mate, and when installing, the tape backing is removed and the panel is positioned on the wall. Permanent support is required.

CONCEALED SPLINES

Panels with concealed spline attachment are provided with kerfs along the edges of the panels. The spline then inserts into one panel and is mounted onto the wall. Adjoining panels are inserted into the remaining half of the spline.

MECHANICAL CLIPS

The panel clips are mounted onto the panels at the time of shipment. The wall clips are installed on the wall at the location established by the position of the panel clips or wall bars.

IMPALING CLIP

The impaling clips are screwed directly to the wall with the prongs extending outward. The glass fiber acoustical panel is positioned and pressed firmly onto the clip. Locking Adhesive is recommended with this clip mounting.

END OF SECTION 09855